HOSTE D BY

Available online at [www.sciencedirect.com](http://www.sciencedirect.com/science/journal/2314808X)


ScienceDirect

journal homepage: <http://ees.elsevier.com/ejbas/default.asp>

[e gypti an j o ur nal o f b a sic and a p p l i ed sci e n c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001)



Full length article

Cloud point extraction of some precious metals using Triton X-114 and a thioamide derivative with a salting-out effect



*Wael I. Mortada* [*a*](#_bookmark0)*,*\**, Mohamed M. Hassanien* [*b*](#_bookmark1)*, Ahmed A. El-Asmy* [*c*](#_bookmark2)

a *Urology and Nephrology Center, Mansoura University, Mansoura, Egypt*

b *Chemistry Department, Industrial Education College, Beni-Suef University, Beni-Suef, Egypt*

c *Chemistry Department, Faculty of Science, Kuwait University, Safat, Kuwait*

## a r t i c l e i n f o

*Article history:*

Received 2 April 2014 Received in revised form 11 July 2014

Accepted 15 July 2014

Available online 10 August 2014

*Keywords:* Palladium Gold Silver

Cloud point extraction Salting-out effect

## a b s t r a c t

A cloud point extraction procedure is proposed for preconcentration of trace amounts of palladium (II), silver (I) and gold (III) in aqueous medium. The metal ions in the initial aqueous solution were extracted using the non-ionic surfactant, Triton X-114 after complex formation with 4-(*p*-chlorophenyl)-1-(pyridin-2-yl)thiosemicarbazide at pH 6.0 in the presence of 0.3 mol L—1 sodium sulfate as a salting-out agent at 25 ◦C. Dilution of the surfactant-rich phase with acidified methanol was performed after phase separa- tion, and the metal ions were determined by electrothermal atomic absorption spec- trometry. The main factors affecting extraction procedure, such as pH, concentration of the ligand, and amount of Triton X-114 were studied in detail. Under the optimum experimental conditions, the calibration graphs were linear upto 125, 50 and 100 mg L—1

and the enrichment factors were 52, 46 and 56 for palladium, silver and gold, respec- tively. The limits of detection, based on three times of standard deviation of blank signal by 10 replicate measurements divided by the slope of calibration curves were

0.12, 0.08 and 0.30 mg L—1 for palladium, silver and gold, respectively. The accuracy of

the results was verified by analyzing spiked water samples. The proposed method has been applied for the determination of the metal ions in soil and rock samples with satisfactory results.

Copyright 2014, Mansoura University. Production and hosting by Elsevier B.V. All rights

reserved.

\* *Corresponding author*. Tel.: +20 1022772144; fax: +20 502263717. E-mail address: [w.mortada@yahoo.com](mailto:w.mortada@yahoo.com) (W.I. Mortada).

Peer review under responsibility of Mansoura University. <http://dx.doi.org/10.1016/j.ejbas.2014.07.001>

2314-808X/Copyright 2014, Mansoura University. Production and hosting by Elsevier B.V. All rights reserved.

[e g ypti an j o ur nal o f b a sic and a pp l i e d sci en c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) 185

# Introduction

Noble metals such as palladium (Pd), silver (Ag) and gold (Au) have many applications in our life [[1,2]](#_bookmark14). These metals occur in the environment at trace and ultratrace levels. Therefore, a very sensitive method is necessary for the accurate and pre- cise determinations. For this purpose, several analytical methods have been developed to measure these ions in real samples including: spectrophotometry, flame atomic absorp- tion spectrometry (FAAS), inductively coupled plasma-mass spectrometry (ICP-MS), inductively coupled plasma-atomic emission spectrometry (ICP-AES), and electrochemical methods.

Electrothermal atomic absorption spectrometry (ETAAS) is

the surfactant-rich phase usually after formation of a hydro- phobic complex with an appropriate chelating agent [[30]](#_bookmark30).

In the present study, we applied CPE for the separation and preconcentration of Pd(II), Ag(I) and Au(III) ions from aqueous solutions by using Triton X-114 as a nonionic surfactant. A thioamide derivative, 4-(*p*-chlorophenyl)-1-(pyridin-2-yl)thio- semicarbazide (HCPTS), was used as the chelating agent. The factors influencing the efficiency of CPE such as effects of pH, Triton X-114, HCPTS concentrations were systematically studied. Also, we introduced a salting-out procedure that en- ables the room temperature phase separation. The developed CPE procedure was successfully applied to determine the concentration of Pd(II), Ag(I) and Au(III) ions in some envi- ronmental samples after the method was validated.

a good technique for the determination of ultra-trace amounts

of heavy metals in several types of samples due to its sensi- tivity. But by reason of ultra-low concentration of metals and high concentration of interfering matrix components in most real samples, ETAAS often requires a suitable pretreatment step.

A number of separation/preconcentration methods have been reported for trace metal determinations: these include solid phase extraction [[3](#_bookmark15)e[6]](#_bookmark15), co-precipitation [[7,8]](#_bookmark16), column extraction [[9,10]](#_bookmark17), ion-selective electrode [[11,12]](#_bookmark18), liquideliquid extraction [[13](#_bookmark19)e[15]](#_bookmark19) and cloud point extraction (CPE) [[16](#_bookmark20)e[26]](#_bookmark20). CPE has attracted a considerable attention because it complies with the “Green Chemistry” principle [[27]](#_bookmark28), as the amount of organic solvent is much less than that of traditional liquid extraction. Moreover, it is simple, cheap, highly efficient, and rapid and of lower toxicity than those used organic solvents. The cloud point is the temperature above which aqueous solutions of non-ionic surfactants become turbid. Specifically, above the cloud point the solution is separated into two phases: a rich phase containing a high surfactant concentra- tion in a small volume and a poor phase with a surfactant concentration close to the critical micelle concentration [[28,29]](#_bookmark29). Accordingly, any metal ions that either directly interact with micelles or after prerequisite binding with hy- drophobic chelating ligand, can be extracted from the parent solution by CPE procedure. Trace elements can be extracted to

# Experimental

### *Reagents and solutions*

All aqueous solutions were prepared with ultrapure water that had been obtained by Milli-Q water purification system (Mil- lipore, Bedford, MA, USA). Reagents used were of analytical grade from SigmaeAldrich (St. Loius, MO, USA) or Merck (Darmstadt, Germany). The laboratory glassware was kept overnight in 10% v/v HNO3 solution. Before the use, the glassware was washed with deionized water and dried in a dust free environment. The standard solutions of Au3+ were

prepared from 1000 mg L—1 Au standard stock solution. The Pd(II) solution was prepared by dissolving 0.1664 g of PdCl2 in 100 mL 0.1 mol L—1 HCl solution and was standardized gravi- metrically by dimethylglyoxime method [[31]](#_bookmark31). A stock solution of 1000 mg L—1 Ag+ was prepared by dissolving 0.1575 g silver nitrate in 0.1 mol L—1 HNO3 and diluting to 100 mL in a volu-

metric flask. It was standardized by using standard NaCl so- lution [[31]](#_bookmark31). Working solutions were freshly prepared from the stock solution by dilutions with deionized water. Triton X-114 was used without further purification. HCPTS was prepared from 2-hydrazinopyridine and *p*-chlorophenylisothiocyanate

as previously reported [[32]](#_bookmark32). One mmol L—1 solution of HCPTS

was prepared by dissolving appropriate amount in 100 mL

ethanol. Buffer solutions were prepared by 1 mol L—1 hydro-

chloric acid e 1 mol L—1 sodium acetate (pH 0.5e3.5);

|  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Table 1 e Instrumental parameters for determination of Pd, Ag and Au using ETAAS. | | | | | | |
| A. Instrumental parameters  Pd | | | | Ag | | Au |
| Wavelength (nm) Slit width (nm) Lamp current (mA) | |  | 247.6  0.2  30 | 328.1  0.7  15 | | 242.8  0.2  15 |
| B. Temperature program  Step Temperature (◦C)  Pd Ag Au | | | | Time (s) Ramp Hold | | Argon flow rate ml/min |
| Drying 1 | 110 |  |  | 1 | 30 | 250 |
| Drying 2 | 130 |  |  | 15 | 30 | 250 |
| Pyrolysis 900 | | 800 | 800 | 15 | 20 | 250 |
| Atomization 2200 | | 1700 | 1800 | 0 | 6 | 0 |
| Cleaning | 2500 |  |  | 1 | 5 | 250 |

0.2 mol L—1 acetic acid e 0.2 mol L—1 sodium acetate (pH 4.0e7.0); 2 mol L—1 ammonium chloride e 2 mol L—1 ammo- nium hydroxide (pH 7.5e10.0).

### *Apparatus*

A Perkin Elmer atomic absorption spectrophotometer (Model AAnalyst 800) with a longitudinal Zeeman background correction furnished with a transversely heated graphite atomizer (THGA) was used for determination of the metal ions. Sample solutions were injected into the atomizer using AS-800 auto sampler. The sample injection volume was 20 mL. The system is equipped with win Lab 32 software. The instru- mental parameters and temperature program for the graphite atomizer were summarized in [Table 1](#_bookmark3). The solution pH was adjusted using Hanna instrument model 8519 digital pH meter. A centrifuge model of CH90-2 (Hinotek Technology Co. Ltd.,

186 [e gypti an j o ur nal o f b a sic and a p p l i ed sci e n c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001)

China) was used to accelerate the phase separation process. A thermostatic bath was operated to reach the cloud point temperature when the room temperature was below 25 ◦C.



Digestion of the geological samples was carried out in a CEM MDS 2000 microwave digestion system (Matthews, NC, USA).

### *Recommended procedure of CPE*

For the CPE, the following procedure was followed: into ali- quots of a solution containing the analyte, add sodium sulfate solution (0.3 mol L—1) to reach the appropriate ionic strength then buffer the solution to pH 6.0. The metal ions were then complexed with HCPTS (5 × 10—5 mol L—1) followed by the addition of Triton X-114 at 0.05% (w/v) concentration. The extraction was carried out at room temperature (25 ◦C). The

phase separation is accelerated by centrifuging at 4000 rpm for 10 min. The phases were cooled down in an ice bath in order to increase the viscosity of the surfactant rich phase. The bulk aqueous phase was decanted by inverting the tube and dried in water bath. The surfactant rich phase in the tube was made up to 1.0 ml by adding mixture of methanol/conc. HNO3 (5:1). The samples were introduced into ETAAS for the determination of the selected metal ions.

### *Preparation of real samples*

* + 1. *Water samples*

The water samples were filtered firstly through filter paper to separate the coarse particles and suspended matter and sec- ondly through a Millipore cellulose nitrate membrane (pore size 0.45 mm), acidified to pH 1 with HNO3 and stored in a refrigerator in a dark polyethylene bottle. 10 ml water sample was subjected to the CPE methodology as described above.

### *Geological samples*

The road dust and rock samples were collected from different area in Sakakah city, Saudi Arabia. The samples were dried at 90 ◦C for 2 h, ground, passed through a sieve of 120 meshes and homogenized. 5 mL of concentrated HNO3, 2 mL of concentrated HF and 2 mL of deionized water were added to

0.5 g of the sample in a Teflon vessel and digested in the mi- crowave digestion oven by applying the heating program shown in [Table 2](#_bookmark5). Finally, 20 mL of 5% w/v boric acid was added, to neutralize excess HF, and the solution was filtered and brought to a final volume of 50 mL with deionized water.

10 ml aliquots of the final clear solution obtained were analyzed by the prescribed procedure.



Fig. 1 e Influence of the pH on the extraction recoveries of Pd, Ag and Au ions. Conditions: 20 mg L¡1 metal ion;

0.3 mol L¡1 Na2SO4; 50 ml aqueous solution;

5 £ 10¡5 mol L¡1 HCPTS; 0.05% w/v Triton X-114; 25 ◦C.

# Result and discussion

### *Optimization of the CPE procedure*

In order to obtain maximum extraction efficiency by CPE method, several parameters need to be taken into account before analysis of the real samples. The most important are:

(1) pH of the sample solution, (2) ligand concentration, (3) surfactant concentration, (4) salting-out effect.

* + 1. *Effect of pH* The pH is a very critical parameter for both the coacervation of the micelles and the complexation of the ligand with the metal ions. The effect of the pH on metal ions extraction was assessed by varying the pH from 1 to 10 by using the suitable buffer. As can be seen from [Fig. 1](#_bookmark4), the optimal extraction ef- ficiency was observed for pH values ranging from 6.0 to 8.0, which is lower than the precipitation of the hydroxide of most transition metals [[33]](#_bookmark33). The optimal extraction is probably due to the formation of a HCPTS neutral complex species at this pH range. This explanation was confirmed by our previous study [[34]](#_bookmark34). For the rest of the optimization process, a pH of 6.0 was used.

### *Effect of ligand concentration*

Chelating reagents are extracted probably due to a specific interaction, such as hydrogen bonding, between functional groups on the chelating reagents and ether oxygen or terminal OH group of the non-ionic surfactant and chelates are extrac- ted into the hydrophobic part of aggregated micelles [[30]](#_bookmark30). In this work, HCPTS was used as a chelating agent because thi- osemicarbazides produce sufficiently hydrophobic complexes with most of transition metals [[34](#_bookmark34)e[37]](#_bookmark34). A 50 mL solution con-

—1

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
| Table 2 e Microwave digestion program for the digestion of the geological samples. | | | | |
| Step | 1 | 2 | 3 | 4 |
| Power (%) | 60 | 60 | 60 | 60 |
| Pressure (psi) | 100 | 130 | 160 | 170 |
| T1a (min) | 30 | 30 | 30 | 30 |
| T2a (min) | 15 | 10 | 5 | 5 |
| T2: time the sample remains at the required pressure.  a T1: maximum time needed to reach the required pressure. | | | | |

taining 20 mgL of the metal ion, 0.05% (w/v) Triton X-114, at a

medium buffer of pH 6.0 containing various amounts of HCPTS (10—6 e 10—4 mol L—1), was subjected to the CPE process. The results are shown in [Fig. 2](#_bookmark6). It can be seen that the extraction

[e g ypti an j o ur nal o f b a sic and a pp l i e d sci en c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) 187





Fig. 2 e Effect of the ligand concentration on the recovery of extraction for Pd, Ag and Au ions. Conditions: 20 mg L¡1 metal ion; 0.3 mol L¡1 Na2SO4; pH, 6.0; 50 ml aqueous solution; 0.05% w/v Triton X-114; 25◦C.

recovery for the metal ions increases with increasing the ligand concentration and remains constant above 5 × 10—5 mol L—1. Therefore, a concentration of 5 × 10—5 mol L—1 of HCPTS was selected as optimal value in this work.

### *Effect of Triton X-114 concentration*

Triton X-114 was chosen because of its commercial avail- ability in a high purified homogeneous form, low toxicological properties and cost. Also, the high density of the surfactant rich phase facilitates phase separation by centrifugation. Additionally, the cloud point (23e26 ◦C) of Triton X-114 per- mits its use in the preconcentration of a large number of molecules and chelates. The variation on the extraction re-

covery, as a function of the Triton X-114 concentration is





Fig. 3 e Effect of the surfactant concentration on the extraction recovery of Pd, Ag and Au ions. Conditions: 20 mg L¡1 metal ions; 0.3 mol L¡1 Na2SO4; pH, 6.0; 50 ml aqueous solution; 5 £ 10¡5 mol L¡1 HCPTS; 25 ◦C.

expressed in [Fig. 3](#_bookmark7), when 50 ml solution containing cations and all the reagents in the presence of 0.01e0.1% (w/v) Triton X-114 was extracted.

As highlighted in [Fig. 3](#_bookmark7), the recovery is maximum as the Triton X-114 concentration was 0.05% (w/v). At lower con- centrations, the extraction efficiency of the complexes was low, due to the inadequacy of the assembly to entrap the complex. Hence, a concentration of 0.05% (w/v) was chosen for further studies.

### *Salting out effect*

Studies on the effects of some additives, such as anionic and non-ionic surfactants and electrolytes, as NaNO3, Na2SO4 and NaCl, on the cloud point behavior of non-ionic surfactants have been reported [[38,39]](#_bookmark35) It was observed that the presence of electrolytes decreases the cloud point (salting-out effect), resulting in a more efficient extraction. The lower cloud point is attributed to electrolytes promoting dehydration of the poly(oxyethylene) chains [[40]](#_bookmark36). According to Hiller et al. [[41]](#_bookmark37) the salting-out phenomenon is directly related to desorption of ions to the hydrophilic parts of the micelles, increasing inter- attraction between micelles and consequently leading to the precipitation of surfactant molecules. Based on this discus- sion, the salting-out effect was studied in both the absence

and presence of different concentrations of NaNO3, Na2SO4 and NaCl (0.05e1 mol L—1 each) at 25 ◦C ([Fig. 4](#_bookmark8)). It was found that Na2SO4 resulted in the highest recovery, and the re- coveries increased with increasing the salt concentration until

reach a maximum at concentration of 0.3 mol L—1. This effect

may be due to the enhanced hydrophobic interactions among the surfactant aggregates and the analyte as well as the decrease in the cloud point temperature of Triton X-114 in the

presence of Na2SO4. At higher concentrations than 0.4 mol L—1,

the signals decreased considerably. High concentration of salt can increase the density of water drops accompanied by the surfactant rich phase, and hence disturb the phase separa- tion. On the other hand, the absence of salt decreased the signal by about 55% (data not shown). This may be due to an

increase in cloud point temperature leading to incomplete phase separation at 25 ◦C. Hence 0.3 M was chosen as the optimum concentration.

### *Analytical performance*

Under the optimum conditions, performance characteristics were obtained by processing standard solutions of Pd(II), Ag(I) and Au(III), and the data is illustrated in [Table 3](#_bookmark9). Calibration functions were linear at least up to 125 mg L—1, 50 mg L—1 and 100 mg L—1, for Pd, Ag and Au, respectively. Furthermore, for preconcentration of 50 ml of the working standard solutions based on the slope ratio of calibration curves with and without preconcentration, an enrichment factor of 52, 46 and 56 was obtained for Pd(II), Ag(I) and Au(III), respectively. To test the reproducibility of the proposed extraction method, the sug-

gested procedure was repeated seven times under optimum conditions. The relative standard deviation (R.S.D.) was measured to be 3.4%, 4.7%, and 2.2% for Pd, Ag and Au, respectively.

Limits of detection (LOD) and quantification (LOQ) for each element were determined according to the expressions at 3 s/

188 [e gypti an j o ur nal o f b a sic and a p p l i ed sci e n c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001)




Fig. 4 e Effect of the addition of different salts on the %recovery of Pd, Ag and Au ions. Conditions: 20 mg L¡1 metal ions; pH, 6.0; 50 ml aqueous solution; 5 £ 10¡5 mol L¡1 HCPTS; 25 ◦C.

m and 10 s/m, respectively (s being, the standard deviation of

10 consecutive blanks and m the slope of the calibration curve). LODs were 0.12 mg L—1 for Pd, 0.08 mg L—1 for Ag and

|  |  |  |  |
| --- | --- | --- | --- |
| Table 3 e Analytical figures of merit for the proposed method. | | | |
| Parameter | Pd(II) | Ag(I) | Au(III) |
| Limit of Detection (mg L—1) | 0.12 | 0.08 | 0.30 |
| Limit of Quantification (mg L—1) | 0.45 | 0.29 | 1.13 |
| Precision (% RSD, C = 20 mg L—1, *n* = 10) | 3.4 | 4.7 | 2.2 |
| Linearity (mg L—1) | 0e125 | 0e50 | 0e100 |
| Correlation Coefficient | 0.998 | 0.997 | 0.995 |
| Enrichment Factor (EF) | 52 | 46 | 56 |
| CPE conditions: 50 mL sample solution, pH 6, 5 × 10—5 mol L—1 HCPTS, 0.05% (w/v) Triton X-114, 0.3 mol L—1 Na2SO4 at 25 ◦C and centrifugation at 4000 RPM for 10 min. | | | |

0.30 mg L—1 for Au and LOQs were 0.45 mg L—1 for Pd, 0.29 mg L—1

for Ag and 1.13 mg L—1 for Au.

### *Effect of the potentially interfering ions*

The efficiency of the suggested method in the extraction and preconcentration of the three ions in the presence of various cationsand anions was examined by usinga solution containing 20 mg L—1 of Pd, Ag and Au with addition of various concentra- tions of potential interferences. The tolerance level was defined

as the maximum amount of foreign species producing an error of ±5% in Pd, Ag and Au determination. The tolerance level of

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Table 4 e Tolerance limits of interfering ions. | | | | | |
| External ion | Tolerable concentration ratio | Pd(II) | %Recovery ±  Ag(I) | S.D. | Au(III) |
| K+ | >1000 | 97.5 ± 2.0 | 96.0 ± 2.4 |  | 99.6 ± 1.0 |
| Na+ | >1000 | 98.2 ± 1.8 | 96.2 ± 2.5 |  | 98.8 ± 2.0 |
| Cs+ | 1000 | 96.4 ± 2.1 | 98.0 ± 1.5 |  | 100.3 ± 2.4 |
| Ca2+ | 1000 | 97.5 ± 1.0 | 99.0 ± 2.1 |  | 101.3 ± 1.0 |
| Mg2+ | 1000 | 99.0 ± 1.5 | 96.2 ± 2.3 |  | 99.6 ± 1.2 |
| Al3+ | 700 | 100.5 ± 2.0 | 97.6 ± 1.6 |  | 99.5 ± 2.6 |
| Bi3+ | 400 | 96.0 ± 2.7 | 98.4 ± 1.0 |  | 98.0 ± 2.7 |
| Fe3+ | 300 | 97.2 ± 1.9 | 99.2 ± 2.1 |  | 96.9 ± 2.4 |
| Fe2+ | 1000 | 97.0 ± 1.8 | 100.0 ± 1.5 |  | 97.4 ± 1.5 |
| Cr3+ | 800 | 97.4 ± 2.3 | 96.3 ± 2.3 |  | 96.6 ± 1.8 |
| Mn2+ | 900 | 96.5 ± 2.0 | 98.3 ± 2.0 |  | 98.5 ± 1.0 |
| Pb2+ | 900 | 102.0 ± 1.8 | 97.6 ± 2.4 |  | 96.8 ± 2.8 |
| Cd2+ | 500 | 97.8 ± 2.2 | 103.0 ± 1.6 |  | 99.0 ± 2.0 |
| Co2+ | 300 | 97.2 ± 2.5 | 98.0 ± 2.0 |  | 95.1 ± 2.5 |
| Ni2+ | 500 | 99.2 ± 1.8 | 97.4 ± 3.0 |  | 103.5 ± 1.2 |
| Zn2+ | 500 | 96.5 ± 2.4 | 96.8 ± 1.9 |  | 95.7 ± 2.0 |
| Hg2+ | 400 | 96.8 ± 3.0 | 95.8 ± 2.5 |  | 95.8 ± 2.3 |
| CrO2- | 1000 | 101.5 ± 1.5 | 98.5 ± 2.0 |  | 99.5 ± 1.8 |
|  |  |  |  |  |  |
| PO3- | 1000 | 98.6 ± 2.0 | 96.4 ± 2.4 |  | 99.9 ± 1.4 |
|  |  |  |  |  |  |
| SCN— | 1000 | 97.4 ± 2.3 | 98.0 ± 1.0 |  | 100.1 ± 2.1 |
| CH3COO— | 1000 | 101.0 ± 1.0 | 96.4 ± 1.6 |  | 97.1 ± 1.6 |
| NO— | 1000 | 99.0 ± 1.8 | 97.0 ± 2.0 |  | 95.5 ± 2.0 |
|  |  |  |  |  |  |
| Tolerance limits of investigated electrolytes is known as ion concentration causing a relative error < ±5% in the sensitivity of method. | | | | | |

[e g ypti an j o ur nal o f b a sic and a pp l i e d sci en c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) 189

LOD (mg L—1)

0.3, 0.5

1.2

7.8

6.0, 0.8

1.4, 1.2

0.7

25.0, 10.0

EF

20.2, 8.6

60

35

40, 35

21, 24

38

28, 35

Reference

[16]

[17]

[18]

[19]

[20]

[21]

[22]

1.6, 1.4

32, 42

[23]

0.12, 0.08, 0.30

52, 46, 56

The present study

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Table 5 e Analysis of Pd, Ag and Au ions in spiked water samples by the proposed method. | | | | | |
| Sample | Ion | Added (mg L—1) | Found (mg L—1) | Recovery (%) | RSD (%) |
| Tape water | Pd(II) | e | N.D. | e | e |
|  |  | 5.0 | 4.95 | 99.0 | 2.5 |
|  |  | 10.0 | 9.92 | 99.2 | 3.2 |
|  | Ag(I) | e | N.D. | e | e |
|  |  | 5.0 | 5.08 | 101.6 | 1.8 |
|  |  | 10.0 | 9.87 | 98.7 | 2.2 |
|  | Au(III) | e | N.D. | e | e |
|  |  | 5.0 | 5.10 | 102.0 | 2.7 |
|  |  | 10.0 | 9.85 | 98.5 | 1.7 |
| River water | Pd(II) | e | N.D. | e | e |
|  |  | 5.0 | 4.88 | 97.6 | 3.1 |
|  |  | 10.0 | 9.75 | 97.5 | 2.6 |
|  | Ag(I) | e | N.D. | e | e |
|  |  | 5.0 | 4.90 | 98.0 | 3.3 |
|  |  | 10.0 | 9.92 | 99.2 | 1.9 |
|  | Au(III) | e | N.D. | e | e |
|  |  | 5.0 | 4.87 | 97.4 | 2.4 |
|  |  | 10.0 | 9.84 | 98.4 | 3.0 |
| Sea water | Pd(II) | e | N.D. | e | e |
|  |  | 5.0 | 5.02 | 100.4 | 2.5 |
|  |  | 10.0 | 10.0 | 100.0 | 2.8 |
|  | Ag(I) | e | N.D. | e | e |
|  |  | 5.0 | 5.11 | 102.2 | 3.3 |
|  |  | 10.0 | 9.90 | 99.0 | 1.5 |
|  | Au(III) | e | N.D. | e | e |
|  |  | 5.0 | 4.89 | 97.8 | 1.8 |
|  |  | 10.0 | 9.66 | 96.6 | 2.3 |
| Results of five determinations of each sample. | | | | | |

each potentially interfering ion species was tested, and if inter- ference occurred, the ratio was reduced until it ceased. As can be seen from [Table 4](#_bookmark10), several species did not interfere even at high concentrations, showing thatthemethoddescribedisapplicable to the analysis of Pd, Ag and Au ions in different samples.

Table 7 e Comparison of the present method with previously reported ones.

Reagent

1,8-diamino-4,5-dihyroxy anthraquinone Ligandless using PONPE 7.5 as a surfactant *O*,*O*-diethyl-dithiophosphate

*O*,*O*-diethyldithiophosphate Ammonium pyrolysine dithiocarbamate dithizone

2-((2-((1H-benzo[d]imidazole-2-yl)methoxy)phenoxy)methyl)-1H-benzo[d]imidazol

Instrument

ICP-OES ETAAS ETAAS

ETV-ICP-MS FAAS

FAAS FAAS

Sample

Mine stones Water

Water and biological samples Biological samples

Soil samples water

waste water, soil and catalyst samples. radiology waste, vegetable, blood and urine samples

Water and geological samples

FAAS

ETAAS

### *Application*

To test the accuracy of the proposed methodology for assaying the metal ions, it is applied for determination of these metal ions in spiked water samples from different sources. The re- coveries of known amounts of Pd, Ag and Au ions added to the samples were examined by the proposed method. The results tabulated in [Table 5](#_bookmark11) show that the recovery of spiked samples is satisfactory reasonable, which indicates the capability of the method in the determination of the metal ions in real samples containing different matrices under the recom- mended conditions. To establish the validity of the proposed method, the described procedure was applied for the

Metal ion

Pd, Au Ag

Ag

Pd, Au Pd, Au Ag

Pd, Ag

Pd, Ag

bis((1H-benzo[d]imidazol-2-yl)ethyl) sulfane

Pd, Ag, Au

HPCTS

|  |
| --- |
| Table 6 e Analysis of Pd, Ag and Au ions in geological samples by the recommended procedure. |
| Samples The present procedure  Pd(II) Ag(I) Au(III) |
| Road dust samples (ng g—1) 29.0 ± 5.3 51.2 ± 5.9 35.5 ± 3.4  Rock samples (ng g—1) 21.1 ± 4.7 73.8 ± 9.2 43.9 ± 6.5 |

190 [e gypti an j o ur nal o f b a sic and a p p l i ed sci e n c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001)

determination of Pd, Ag and Au in dust and rock samples. The obtained results were summarized in [Table 6](#_bookmark12).

# Conclusion

The lipophilicity of HCPTS and its tolerance for the in- terferences caused by the co-existing metal ions make it feasible for CPE and selective towards Pd, Ag and Au. It permits the separation process at room temperature with the aid of salting-out effect. Compared with traditional CPE (about 40 min for heating, incubation and cooling), the extraction time of the proposed method was very short (a few minutes). The developed procedure yielded good results in terms of selectivity, accuracy and precision for the rapid determination of Pd, Ag and Au in real samples. The pro- posed methodology was compared to other CPE methods reported recently in the literature [[16](#_bookmark20)e[23]](#_bookmark20). The distinct fea- tures are summarized in [Table 7](#_bookmark13). As can be seen, our results are comparable with, and in some cases better than, the reported ones.

## references

1. [Hartley FR. Chemistry of the platinum group metals.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref1) [Amsterdam: Elsevier; 1991](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref1).
2. [Green Wood NN, Earnshaw A. Chemistry of the elements.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref2) [2nd ed. Oxford: Buttewirth Heinemann; 1997](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref2).
3. [Wu Y, Jiang Z, Hu B, Duan J. Electrothermal vaporization](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3) [inductively coupled plasma atomic emission spectrometry](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3) [determination of gold, palladium, and platinum using](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3) [chelating resin YPA4 as both extractant and chemical](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3) [modifier. Talanta 2004;63:585](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3)e[92](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref3).
4. [Qing Y, Hang Y, Wanjaul R, Jiang Z, Hu B. Adsorption](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref4) [behavior of Noble metal ions (Au, Ag, Pd) on nanometer-size](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref4) [titanium dioxide with ICP-AES. Anal Sci 2003;19:1417](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref4)e[20](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref4).
5. [Yin P, Xu Q, Qu R, Zhao G, Sun Y. Adsorption of transition](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref5) [metal ions from aqueous solutions onto a novel silica gel](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref5) [matrix inorganic-organic composite material. J Hazard Mater](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref5) [2010;173:710](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref5)e[6](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref5).
6. [Chand R, Watari T, Inoue K, Kawakita H, Luitel HN,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6) [Parajuli D, et al. Selective adsorption of precious metal](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6) [from hydrochloric acid solutions using porous carbon](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6) [prepared from barley straw and rice husk. Miner Eng](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6) [2009;22:1277](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6)e[82](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref6).
7. [Soylak M, Tuzen M. Coprecipitation of gold(III), palladium(II)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref7) [and lead(II) for their flame atomic absorption spectrometric](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref7) [determinations. J Hazard Mater 2008;152:656](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref7)e[61](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref7).
8. [Sawant SS. Sequential separation and spectrophotometric](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref8) [determination of osmium and platinum with 5-chloro-2-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref8) [hydroxythiobenzhydrazide. Anal Sci 2009;25:813](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref8)e[8](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref8).
9. [Hu Q, Yang X, Huang Z, Chen J, Yang G. Simultaneous](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9) [determination of palladium, platinum, rhodium and gold by](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9) [on-line solid phase extraction and high performance liquid](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9) [chromatography with 5-(2-hydroxy-5-nitrophenylazo)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9) [thiorhodanine as pre-column derivatization regents. J](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9) [Chromatogr A 2005;1094:77](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9)e[82](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref9).
10. [S](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10)a´[nchez JM, Obrezkov O, Salvad](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10)o´ [V. Separation of some](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10) [platinum group metal chelates with 8-hydroxyquinoline by](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10) [various high-performance liquid chromatographic methods.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10) [J Chromatogr A 2000;871:217](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10)e[26](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref10).
11. [Gholivand MB, Mohammadi M, Khodadadian M, Rofouei MK.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref11) [Novel Platinum(II) Selective Membrane Electrode Based on](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref11) [1,3-bis(2-cyanobenzene)triazene. Talanta 2009;78:922](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref11)e[8](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref11).
12. [Gupta VK, Goyal RN, Sharma RA. Comparative studies of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref12) [ONNO-based ligands as ionophores for palladium ion-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref12) [selective membrane sensors. Talanta 2009;78:484](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref12)e[90](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref12).
13. [Kagaya S, Takata D, Yoshimori T, Kanbara T, Tohda K. A](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13) [sensitive and selective method for determination of gold(III)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13) [based on electrothermal atomic absorption spectrometry in](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13) [combination with dispersive liquid](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13)e[liquid microextraction](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13) [using dicyclohexylamine. Talanta 2010;80:1364](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13)e[70](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref13).
14. [Park YJ, Fray DJ. Recovery of high purity precious metals](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref14) [from printed circuit boards. J Hazard Mater 2009;164:1152](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref14)e[8](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref14).
15. [Pan L, de Zhang Z. Solvent extraction and separation of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref15) [palladium(II) and platinum(IV) from hydrochloric acid](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref15) [medium with dibutyl sulfoxide. Miner Eng 2009;22:1271](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref15)e[6](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref15).
16. [Tavakoli L, Yamini Y, Ebrahimzadeh H, Nezhadali A,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16) [Shariati S, Nourmohammadi F. Development of cloud point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16) [extraction for simultaneous extraction and determination of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16) [gold and palladium using ICP-OES. J Hazard Mat](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16) [2008;152:737](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16)e[43](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref16).
17. [Manzoori JL, Abdolmohammad-Zadeh H, Amjadi M. Ultra-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17) [trace determination of silver in water samples by](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17) [electrothermal atomic absorption spectrometry after](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17) [preconcentration with a ligand-less cloud point extraction](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17) [methodology. J Hazard Mater 2007;144:458](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17)e[63](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref17).
18. [Fan Z, Bai F. Determination of trace amounts of silver in](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref18) [various samples by electrothermal atomic absorption](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref18) [spectrometry after sample preparation using cloud point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref18) [extraction. At Spectrosc 2007;28:30](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref18)e[4](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref18).
19. [da Silva M, Frescura V, Curtius A. Determination of noble](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19) [metals in biological samples by electrothermal](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19) [vaporization inductively coupled plasma mass](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19) [spectrometry, following cloud point extraction.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19) [Spectrochim Acta B 2001;56:1941](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19)e[9](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref19).
20. [Lian Y, Zhen W, Tai Z, Yang Y, Song J, Li Z. Cloud point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref20) [extraction and flame atomic absorption spectrometry](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref20) [analysis of palladium, platinum, and gold ions from](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref20) [industrial polluted soil. Rare Met 2012;31:512](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref20)e[6](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref20).
21. [Dalali N, Javadi N, Agrawal YK. On-line incorporation of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref21) [cloud point extraction in flame atomic absorption](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref21) [spectrometric determination of silver. Turk J Chem](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref21) [2008;32:561](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref21)e[70](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref21).
22. [Tavallali H, Yazdandoust S, Yazdandoust M. Cloud Point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22) [extraction for the preconcentration of silver and palladium](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22) [in real samples and determination by atomic absorption](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22) [spectrometry. Clean](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22) e [soil, Air, Water 2010;38:242](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22)e[7](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref22).
23. [Ghaedi M, Shokrollahi A, Niknam K, Niknam E, Najibi A,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23) [Soylak M. Cloud point extraction and flame atomic](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23) [absorption spectrometric determination of cadmium(II),](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23) [lead(II), palladium(II) silver(I) environ samples. J Hazard](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23) [Mater 2009;168:1022](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23)e[7](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref23).
24. [Mortada WI, Ali AZ, Hassanien MM. Mixed micelle-mediated](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24) [extraction of alizarin red S complexes of Zr(IV) and Hf(IV)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24) [ions prior to their determination by inductively coupled](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24) [plasma-optical emission spectrometry. Anal Meth](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24) [2013;5:5234](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24)e[40](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref24).
25. [Mortada WI, Hassanien MM, El-Asmy AA. Speciation of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref25) [platinum in blood plasma and urine by micelle-mediated](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref25) [extraction and graphite furnace atomic absorption](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref25) [spectrometry. J Trace Elem Med Biol 2013;27:267](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref25)e[72](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref25).
26. [Mortada WI, Hassanien MM, El-Asmy AA. Cloud point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref26) [extraction for the determination of trace amounts of Pt(IV)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref26) [by graphite furnace atomic absorption spectrometry. Anal](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref26) [Meth 2013;5:530](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref26)e[5](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref26).
27. [Anastas P, Eghbali N. Green chemistry: principles and](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref27) [Practice, Chem. Soc Rev 2010;39:301](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref27)e[12](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref27).

[e g ypti an j o ur nal o f b a sic and a pp l i e d sci en c e s 1 ( 2014) 184](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) e[191](http://dx.doi.org/10.1016/j.ejbas.2014.07.001) 191

1. [Ghaedi M, Shokrollahi A, Niknam K, Niknam E, Derki S,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28) [Soylak MA. Cloud point extraction procedure for](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28) [preconcentration/flame atomic absorption spectro-metric](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28) [determination of silver, zinc, and lead at sub-trace levels in](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28) [environmental samples. J AOAC Int 2009;92:907](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28)e[13](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref28).
2. [Filik H, Cengel T, Apak R. Determination of molybdenum (VI)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref29) [ion in seawater samples. J Hazard Mater 2009;169:766](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref29)e[71](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref29).
3. [Ojeda CB, Rojas FS. Separation and preconcentration by a](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref30) [cloud Point extraction procedure for determination of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref30) [metals: an overview. Anal Bioanal Chem 2009;394:759](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref30)e[82](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref30).
4. [Jeffery GH, Bassett J, Mendham J, Denney RC. Vogel's](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref31) [textbook of quantitative chemical analysis. 5th ed. New](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref31) [York: Longman Scientific and Technical; 1989](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref31).
5. [Hassanien MM, Hassan AM, Mortada WI, El-Asmy AA. A new](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref32) [thioamide derivative for separation and preconcentration of](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref32) [multi elements in aquatic environment by cloud point](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref32) [extraction. Am J Anal Chem 2011;2:697](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref32)e[709](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref32).
6. [Schweitzer GK, Pesterfield LL. The aqueous chemistry of the](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref33) [elements. New York: Oxford University Press; 2010](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref33).
7. [Hassanien MM, Mortada WI, Hassan AM, El-Asmy AA.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref34) [Synthesis, characterization and biological activities of 4-(*p*-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref34) [chlorophenyl)-1-(pyridin-2-yl)thiosemicarbazide and its](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref34) [metal complexes. J Korean Chem Soc 2012;56:679](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref34)e[91](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref34).
8. [Hassanien MM, Gabr IM, Abdel-Rhman MH, El-Asmy AA.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35) [Synthesis and structural investigation of mono and](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35) [polynuclear copper complexes of 4-ethyl-1-(pyridin-2-yl)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35)

[thiosemicarbazide. Spectrochim Acta A Mol Biomol](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35) [Spectrosc 2008;71:73](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35)e[9](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref35).

1. [El-Asmy AA, Al-Gammal OA, Saad DA, Ghazy SE. Synthesis,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref36) [characterization, molecular modeling and eukaryotic DNA](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref36) [degradation of 1-(3,4-dihydroxybenzylidene)](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref36) [thiosemicarbazide complexes. J Mol Struct 2009;934:9](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref36)e[22](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref36).
2. [El-Asmy AA, Al-Ansi TY, Amin RR, Mounir M. Spectral,](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref37) [magnetic and electrical properties of 1-succinyl bis(4-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref37) [phenylthiosemicarbazide) complexes. Polyhedron](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref37) [2009;9:2029](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref37)e[34](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref37).
3. [Hinze WL, Pramauro E. Critical review of surfactant-](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref38) [mediated phase separation (cloud-point extractions): theory](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref38) [and applications. Crit Rev Anal Chem 1993;24:133](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref38)e[77](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref38).
4. [Nascentes CC, Arruda MAZ. Cloud point formation based on](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref39) [mixed micelles in the presence of electrolytes for cobalt](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref39) [extraction and preconcentration. Talanta 2003;61:759](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref39)e[68](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref39).
5. [Armstrong JK, Chowdhry BZ, Snowden MJ, Leharne SA. Effect](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40) [of sodium chloride upon micellization and phase separation](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40) [transitions in aqueous solutions of triblock copolymers:](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40) [a](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40) [high-sensitivity differential scanning calorimetry study.](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40) [Langmuir 1998;14:2004](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40)e[10](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref40).
6. [Komaromy-Hiller G, Calkins N, Wandruszka R. Changes in](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41) [polarity and aggregation number upon clouding of a](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41) [nonionic detergent:](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41) [effect of ionic surfactants and sodium](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41) [chloride. Langmuir 1996;12:916](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41)e[20](http://refhub.elsevier.com/S2314-808X(14)00029-3/sref41).